Peer review AMG v95

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SV72T_50FL.amg | Stopray Vision 72T 5.0mm | Asahimas | 4.880 | 1406 | Coated | Front | 0.381 | 0.500 | 0.401 | 0.802 | 0.093 | 0.098 | 0.027 | 0.840 |