Peer review JJG v95

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Optilite US1.16_12.JJG | Optilite US1.16_12 | Shandong Jinjing Science&technology Stock co., LTD | 11.830 | 17640 | Coated | Back | 0.633 | 0.214 | 0.277 | 0.890 | 0.065 | 0.053 | 0.843 | 0.073 |