Peer review EFG v95

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| NE 80_6.EFG | Emicool Plus T NE 80 6mm | Emirates Float Glass.LLC | 5.700 | 28763 | Coated | Back | 0.565 | 0.199 | 0.256 | 0.824 | 0.091 | 0.059 | 0.840 | 0.047 |