Peer review WMG v95

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 5mmSL185.WMG | 5mmSL185 | Wangmei Industrial Group Co., Ltd | 4.920 | 29020 | Coated | Back | 0.581 | 0.207 | 0.267 | 0.852 | 0.068 | 0.049 | 0.843 | 0.081 |