Peer review CIG v95

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Clr-3_030Gry_060PVB_Clr-3.CIG | Clear-3 / .030 Grey PVB / .060 PVB / Clear-3 | Cardinal Glass Industries | 8.290 | 18310 | Laminate | Neither | 0.459 | 0.052 | 0.052 | 0.427 | 0.052 | 0.052 | 0.840 | 0.840 |