Peer review SYP v95

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| YST0680T_6HT.syp | Curved Tempered LowE on Low Iron #2 side | SYP GLASS GROUP CO.,LTD | 6.000 | 8417 | Coated | Back | 0.623 | 0.191 | 0.224 | 0.843 | 0.052 | 0.047 | 0.840 | 0.103 |
| YST0680T_8HT.syp | Curved Tempered LowE on Low Iron #2 side | SYP GLASS GROUP CO.,LTD | 8.000 | 8418 | Coated | Back | 0.618 | 0.184 | 0.222 | 0.838 | 0.052 | 0.047 | 0.840 | 0.117 |