Peer review TTA v95

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CLR-PTE71A-6-HS.TTA | CLR-PTE71A-6-HS | TG Taicang Architectural Glass Co. , Ltd | 5.860 | 28856 | Coated | Back | 0.308 | 0.337 | 0.494 | 0.708 | 0.057 | 0.068 | 0.844 | 0.050 |