Peer review VIR v95

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| VE26-85-6.VIR | VE-85 on SolarBlue | Viracon | 5.660 | 6434 | Coated | Back | 0.349 | 0.079 | 0.218 | 0.531 | 0.052 | 0.036 | 0.840 | 0.088 |