Peer review VTA v95

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SB65 Clear_6.VTA | Solarban® 65 on Clear 6mm | Vitro formerly PPG | 5.664 | 5300 | Coated | Back | 0.354 | 0.315 | 0.508 | 0.779 | 0.092 | 0.082 | 0.840 | 0.028 |
| SB65 Clear_8.VTA | Solarban® 65 on Clear 8mm | Vitro formerly PPG | 7.925 | 5301 | Coated | Back | 0.343 | 0.266 | 0.508 | 0.768 | 0.090 | 0.081 | 0.840 | 0.028 |
| SB65 Clear_10.VTA | Solarban® 65 on Clear 10mm | Vitro formerly PPG | 9.398 | 5302 | Coated | Back | 0.337 | 0.240 | 0.507 | 0.762 | 0.090 | 0.081 | 0.840 | 0.028 |
| SB65 Acuity_6.VTA | Solarban® 65 on Acuity® 6mm | Vitro formerly PPG | 5.664 | 5303 | Coated | Back | 0.371 | 0.411 | 0.509 | 0.795 | 0.093 | 0.083 | 0.840 | 0.028 |
| SB65 Acuity_8.VTA | Solarban® 65 on Acuity® 8mm | Vitro formerly PPG | 7.925 | 5304 | Coated | Back | 0.366 | 0.379 | 0.509 | 0.790 | 0.093 | 0.083 | 0.840 | 0.028 |
| SB65 Acuity_10.VTA | Solarban® 65 on Acuity® 10mm | Vitro formerly PPG | 9.398 | 5305 | Coated | Back | 0.363 | 0.360 | 0.509 | 0.787 | 0.093 | 0.083 | 0.840 | 0.028 |
| SB65 Starphire_6.VTA | Solarban® 65 on Starphire® 6mm | Vitro formerly PPG | 5.664 | 5306 | Coated | Back | 0.379 | 0.468 | 0.509 | 0.801 | 0.094 | 0.084 | 0.840 | 0.028 |
| SB65 Starphire_8.VTA | Solarban® 65 on Starphire® 8mm | Vitro formerly PPG | 7.925 | 5307 | Coated | Back | 0.377 | 0.453 | 0.509 | 0.798 | 0.094 | 0.083 | 0.840 | 0.028 |
| SB65 Starphire_10.VTA | Solarban® 65 on Starphire® 10mm | Vitro formerly PPG | 9.398 | 5308 | Coated | Back | 0.375 | 0.444 | 0.509 | 0.796 | 0.094 | 0.083 | 0.840 | 0.028 |