Peer review AGC v100

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LQT5G.AGC | Low-E Aqua Green T 5mm | AGC ASAHI GLASS CO., LTD. | 4.730 | 15016 | Coated | Front | 0.384 | 0.492 | 0.376 | 0.800 | 0.079 | 0.079 | 0.022 | 0.846 |
| LPT5G.AGC | Low-E Pure Clear T 5mm | AGC ASAHI GLASS CO., LTD. | 4.730 | 15017 | Coated | Front | 0.587 | 0.298 | 0.239 | 0.864 | 0.061 | 0.079 | 0.044 | 0.846 |
| LLT4G.AGC | Low-E Light Clear T 4mm | AGC ASAHI GLASS CO., LTD. | 3.750 | 15018 | Coated | Front | 0.567 | 0.339 | 0.278 | 0.871 | 0.062 | 0.077 | 0.036 | 0.848 |
| LLT5G.AGC | Low-E Light Clear T 5mm | AGC ASAHI GLASS CO., LTD. | 4.730 | 15019 | Coated | Front | 0.565 | 0.328 | 0.256 | 0.868 | 0.059 | 0.075 | 0.040 | 0.846 |