Peer review GRE v100

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HPAmber4129_6.gre | SunGuard HP Amber 41/29 on Float ExtraClear 6mm | Guardian Europe | 5.842 | 11853 | Coated | Back | 0.260 | 0.371 | 0.426 | 0.443 | 0.230 | 0.122 | 0.840 | 0.051 |
| HPAmber4129_8.gre | SunGuard HP Amber 41/29 on Float ExtraClear 8mm | Guardian Europe | 7.747 | 11854 | Coated | Back | 0.257 | 0.354 | 0.426 | 0.441 | 0.228 | 0.122 | 0.840 | 0.050 |
| HPAmber4129_10.gre | SunGuard HP Amber 41/29 on Float ExtraClear 10mm | Guardian Europe | 9.754 | 11855 | Coated | Back | 0.247 | 0.326 | 0.430 | 0.431 | 0.226 | 0.127 | 0.840 | 0.049 |
| HPAmber4129_UC10.gre | SunGuard HP Amber 41/29 on Float UltaClear 10mm | Guardian Europe | 9.754 | 11856 | Coated | Back | 0.270 | 0.415 | 0.428 | 0.446 | 0.234 | 0.124 | 0.840 | 0.048 |