Peer review GPP v100

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Clear2mm.gpp | Clear2mm | Gutmann PVB Plastic Sheets Manufacturing LLC | 1.869 | 0 | Monolithic | Neither | 0.863 | 0.073 | 0.073 | 0.913 | 0.078 | 0.078 | 0.840 | 0.840 |
| Extra Clear pvb 0.38mm.gpp | Extra Clear pvb 0.38mm | Gutmann PVB Plastic Sheets Manufacturing LLC | 4.137 | 29100 | Laminate | Neither | 0.807 | 0.075 | 0.075 | 0.895 | 0.084 | 0.084 | 0.840 | 0.840 |
| Extra Clear pvb 0.76mm.gpp | Extra Clear pvb 0.76mm | Gutmann PVB Plastic Sheets Manufacturing LLC | 4.519 | 29101 | Laminate | Neither | 0.775 | 0.071 | 0.071 | 0.894 | 0.081 | 0.081 | 0.840 | 0.840 |
| Extra Clear pvb 1.14mm.gpp | Extra Clear pvb 1.14mm | Gutmann PVB Plastic Sheets Manufacturing LLC | 4.843 | 29102 | Laminate | Neither | 0.764 | 0.072 | 0.072 | 0.892 | 0.084 | 0.084 | 0.840 | 0.840 |
| Extra Clear pvb 1.52mm.gpp | Extra Clear pvb 1.52mm | Gutmann PVB Plastic Sheets Manufacturing LLC | 5.221 | 29103 | Laminate | Neither | 0.738 | 0.069 | 0.069 | 0.884 | 0.080 | 0.080 | 0.840 | 0.840 |