Peer review SGG v100

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CL SKN 183 II 4mm PLX.SGG | SGG COOL-LITE SKN 183 II 4mm PLX | Saint-Gobain Glass | 4.000 | 20912 | Coated | Back | 0.371 | 0.366 | 0.452 | 0.819 | 0.063 | 0.057 | 0.845 | 0.022 |
| CL SKN 183 II 5mm PLX.SGG | SGG COOL-LITE SKN 183 II 5mm PLX | Saint-Gobain Glass | 5.000 | 20913 | Coated | Back | 0.369 | 0.351 | 0.451 | 0.815 | 0.063 | 0.056 | 0.845 | 0.021 |
| CL SKN 183 II 6mm PLX.SGG | SGG COOL-LITE SKN 183 II 6mm PLX | Saint-Gobain Glass | 6.000 | 20914 | Coated | Back | 0.366 | 0.337 | 0.451 | 0.812 | 0.063 | 0.056 | 0.845 | 0.019 |
| CL SKN 183 II 8mm PLX.SGG | SGG COOL-LITE SKN 183 II 8mm PLX | Saint-Gobain Glass | 8.000 | 20915 | Coated | Back | 0.359 | 0.310 | 0.451 | 0.805 | 0.062 | 0.055 | 0.846 | 0.019 |
| CL SKN 183 II 10mm PLX.SGG | SGG COOL-LITE SKN 183 II 10mm PLX | Saint-Gobain Glass | 10.000 | 20916 | Coated | Back | 0.354 | 0.287 | 0.450 | 0.798 | 0.062 | 0.055 | 0.845 | 0.019 |
| COOL-LITE SKN 152 II 6mm.SGG | SGG COOL-LITE SKN 152 II 6mm | Saint-Gobain Glass | 6.000 | 20918 | Coated | Back | 0.229 | 0.375 | 0.418 | 0.543 | 0.154 | 0.071 | 0.845 | 0.017 |
| COOL-LITE SKN 152 II 8mm.SGG | SGG COOL-LITE SKN 152 II 8mm | Saint-Gobain Glass | 8.000 | 20919 | Coated | Back | 0.226 | 0.348 | 0.418 | 0.538 | 0.152 | 0.071 | 0.846 | 0.017 |
| COOL-LITE SKN 152 II 10mm .SGG | SGG COOL-LITE SKN 152 II 10mm | Saint-Gobain Glass | 10.000 | 20920 | Coated | Back | 0.223 | 0.324 | 0.418 | 0.534 | 0.150 | 0.071 | 0.845 | 0.016 |
| CL XTREME 70-33II 4mm.SGG | SGG COOL-LITE XTREME 70-33 II 4mm | Saint-Gobain Glass | 4.000 | 21059 | Coated | Back | 0.297 | 0.411 | 0.544 | 0.772 | 0.059 | 0.057 | 0.840 | 0.018 |