Peer review GRD v103

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SGSNR50C5.grd | SunGuard® SNR 50 on 5mm Clear | Guardian | 4.623 | 26291 | Coated | Back | 0.242 | 0.419 | 0.517 | 0.534 | 0.237 | 0.102 | 0.840 | 0.029 |