Peer review TTA v103

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SCL-PTGY6-6mm.TTA | SCL-PTGY6-6mm | TG Taicang Architectural Glass Co. , Ltd | 5.860 | 28862 | Coated | Back | 0.243 | 0.480 | 0.508 | 0.590 | 0.097 | 0.080 | 0.843 | 0.032 |