Peer review MMM v103

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CA35.mmm | Ceramic Archtectural 35 | 3M Corporation | 3.352 | 2819 | Applied Film | Back | 0.241 | 0.050 | 0.051 | 0.383 | 0.055 | 0.056 | 0.840 | 0.903 |
| CA45.mmm | Ceramic Architectural 45 | 3M Corporation | 3.352 | 2820 | Applied Film | Back | 0.281 | 0.055 | 0.051 | 0.460 | 0.062 | 0.060 | 0.840 | 0.904 |
| CA60.mmm | Ceramic Architectural 60 | 3M Corporation | 3.352 | 2821 | Applied Film | Back | 0.356 | 0.059 | 0.057 | 0.634 | 0.072 | 0.070 | 0.840 | 0.903 |
| CA80.mmm | Ceramic Architectural 80 | 3M Corporation | 3.352 | 2822 | Applied Film | Back | 0.435 | 0.062 | 0.063 | 0.790 | 0.081 | 0.081 | 0.840 | 0.906 |