Peer review SAG v103

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RealTone SR2 9mm Clear.SAG | SageGlass® RealTone™ SR2 9mm Lami Clear Tint | SAGE Electrochromics, Inc. | 8.660 | 8940 | Laminate | Back | 0.358 | 0.115 | 0.122 | 0.649 | 0.097 | 0.074 | 0.841 | 0.163 |
| RealTone SR2 9mm Light.SAG | SageGlass® RealTone™ SR2 9mm Lami Light Tint | SAGE Electrochromics, Inc. | 8.660 | 8941 | Laminate | Back | 0.090 | 0.127 | 0.089 | 0.203 | 0.108 | 0.019 | 0.841 | 0.163 |
| RealTone SR2 9mm Medium.SAG | SageGlass® RealTone™ SR2 9mm Lami Medium Tint | SAGE Electrochromics, Inc. | 8.660 | 8942 | Laminate | Back | 0.026 | 0.117 | 0.087 | 0.061 | 0.100 | 0.013 | 0.841 | 0.163 |
| RealTone SR2 9mm Full.SAG | SageGlass® RealTone™ SR2 9mm Lami Full Tint | SAGE Electrochromics, Inc. | 8.660 | 8943 | Laminate | Back | 0.004 | 0.127 | 0.091 | 0.011 | 0.107 | 0.013 | 0.841 | 0.163 |
| RealTone STBS 9mm Clear.SAG | SageGlass® RealTone™ STBS 9mm Lami Clear Tint | SAGE Electrochromics, Inc. | 8.760 | 8944 | Laminate | Back | 0.350 | 0.183 | 0.140 | 0.599 | 0.173 | 0.116 | 0.841 | 0.163 |
| RealTone STBS 9mm Light.SAG | SageGlass® RealTone™ STBS 9mm Lami Light Tint | SAGE Electrochromics, Inc. | 8.760 | 8945 | Laminate | Back | 0.078 | 0.180 | 0.091 | 0.173 | 0.174 | 0.023 | 0.841 | 0.163 |
| RealTone STBS 9mm Medium.SAG | SageGlass® RealTone™ STBS 9mm Lami Medium Tint | SAGE Electrochromics, Inc. | 8.760 | 8946 | Laminate | Back | 0.026 | 0.179 | 0.090 | 0.060 | 0.172 | 0.015 | 0.841 | 0.163 |
| RealTone STBS 9mm Full.SAG | SageGlass® RealTone™ STBS 9mm Lami Full Tint | SAGE Electrochromics, Inc. | 8.760 | 8947 | Laminate | Back | 0.004 | 0.179 | 0.092 | 0.010 | 0.173 | 0.014 | 0.841 | 0.163 |
| RealTone Gray 9mm Clear.SAG | SageGlass® RealTone™ Gray 9mm Lami Clear Tint | SAGE Electrochromics, Inc. | 8.660 | 8948 | Laminate | Back | 0.273 | 0.074 | 0.104 | 0.503 | 0.052 | 0.032 | 0.841 | 0.163 |
| RealTone Gray 9mm Light.SAG | SageGlass® RealTone™ Gray 9mm Lami Light Tint | SAGE Electrochromics, Inc. | 8.660 | 8949 | Laminate | Back | 0.067 | 0.070 | 0.080 | 0.153 | 0.050 | 0.015 | 0.841 | 0.163 |
| RealTone Gray 9mm Medium.SAG | SageGlass® RealTone™ Gray 9mm Lami Medium Tint | SAGE Electrochromics, Inc. | 8.660 | 8950 | Laminate | Back | 0.018 | 0.070 | 0.088 | 0.044 | 0.050 | 0.016 | 0.841 | 0.163 |
| RealTone Gray 9mm Full.SAG | SageGlass® RealTone™ Gray 9mm Lami Full Tint | SAGE Electrochromics, Inc. | 8.660 | 8951 | Laminate | Back | 0.003 | 0.071 | 0.091 | 0.008 | 0.050 | 0.014 | 0.841 | 0.163 |