Peer review SGG v103

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| COOL-LITE KN 453 II 5mm.SGG | SGG COOL-LITE KN 453 II 5mm | Saint-Gobain Glass | 5.000 | 21188 | Coated | Back | 0.222 | 0.101 | 0.311 | 0.441 | 0.095 | 0.059 | 0.840 | 0.058 |