Peer review AFT v104

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Clear Float 4mm.AFT | Clear Float 4mm | AGC Flat Glass (Thailand) | 3.910 | 19009 | Monolithic | Neither | 0.828 | 0.076 | 0.077 | 0.895 | 0.084 | 0.084 | 0.840 | 0.840 |
| Clear Float 5mm.AFT | Clear Float 5mm | AGC Flat Glass (Thailand) | 4.930 | 19010 | Monolithic | Neither | 0.817 | 0.075 | 0.075 | 0.892 | 0.082 | 0.082 | 0.840 | 0.840 |
| Clear Float 6mm.AFT | Clear Float 6mm | AGC Flat Glass (Thailand) | 5.910 | 19011 | Monolithic | Neither | 0.788 | 0.073 | 0.075 | 0.884 | 0.083 | 0.083 | 0.840 | 0.840 |
| Clear Float 10mm.AFT | Clear Float 10mm | AGC Flat Glass (Thailand) | 9.680 | 19012 | Monolithic | Neither | 0.716 | 0.069 | 0.071 | 0.863 | 0.081 | 0.082 | 0.840 | 0.840 |