Peer review WHG v104

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6mm SGR168 on Clear.WHG | 6mm SGR168 on Clear | BEIJING WUHUATIANBAO GLASS CO.,LTD | 5.780 | 17497 | Coated | Back | 0.382 | 0.173 | 0.352 | 0.682 | 0.058 | 0.055 | 0.845 | 0.051 |
| 6mm WT1.16 on Clear.WHG | 6mm WT1.16 on Clear | BEIJING WUHUATIANBAO GLASS CO.,LTD | 5.860 | 17498 | Coated | Back | 0.593 | 0.189 | 0.262 | 0.876 | 0.054 | 0.043 | 0.843 | 0.064 |
| 3mm WFT50 on Clear.WHG | 3mm WFT50 on Clear | BEIJING WUHUATIANBAO GLASS CO.,LTD | 2.850 | 17499 | Coated | Back | 0.223 | 0.399 | 0.449 | 0.540 | 0.079 | 0.071 | 0.844 | 0.046 |