Peer review AIS v104

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dark Grey Lite Plus_6.AIS | Dark Grey Lite Plus | Asahi India Glass Limited | 6.121 | 17051 | Coated | Front | 0.098 | 0.368 | 0.086 | 0.099 | 0.096 | 0.045 | 0.051 | 0.840 |