Peer review GTS v104

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CNeutral60_EF4.GTS | COMBI Neutral 60 on Clear EUROFLOAT 4 mm | Glas Trösch AG | 3.800 | 14881 | Coated | Front | 0.300 | 0.480 | 0.402 | 0.667 | 0.053 | 0.095 | 0.031 | 0.840 |