Peer review NSG v105

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SuncoolOptilam7040_12.8mm.nsg | Suncool Optilam 70/40 12.8mm | Pilkington | 12.670 | 4174 | Laminate | Back | 0.366 | 0.206 | 0.424 | 0.766 | 0.051 | 0.037 | 0.846 | 0.042 |