Peer review AFT v105

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Clear Float 3mm.AFT | Clear Float 3mm | AGC Flat Glass (Thailand) | 2.780 | 19013 | Monolithic | Neither | 0.848 | 0.078 | 0.078 | 0.899 | 0.084 | 0.084 | 0.840 | 0.840 |
| Clear Float 3.2mm.AFT | Clear Float 3.2mm | AGC Flat Glass (Thailand) | 3.160 | 19014 | Monolithic | Neither | 0.844 | 0.078 | 0.078 | 0.899 | 0.084 | 0.084 | 0.840 | 0.840 |
| Clear Float 8mm.AFT | Clear Float 8mm | AGC Flat Glass (Thailand) | 7.580 | 19015 | Monolithic | Neither | 0.768 | 0.072 | 0.072 | 0.879 | 0.081 | 0.081 | 0.840 | 0.840 |
| Clear Float 12mm.AFT | Clear Float 12mm | AGC Flat Glass (Thailand) | 11.430 | 19016 | Monolithic | Neither | 0.699 | 0.068 | 0.068 | 0.861 | 0.079 | 0.080 | 0.840 | 0.840 |