Peer review SAF V105

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SLIIXL60IGU_C-0063084.SAF | SuperLite II-XL 60 Custom C-0063084 | SAFTI FIRST Fire Rated Glazing Solutions | 61.000 | 16606 | Laminate | Neither | 0.086 | 0.083 | 0.494 | 0.235 | 0.086 | 0.178 | 0.845 | 0.843 |