Peer review LOF v105

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| OptiViewOW6.LOF | OptiView™ on Optiwhite™ | Pilkington North America | 5.910 | 10001 | Coated | Front | 0.852 | 0.063 | 0.065 | 0.922 | 0.053 | 0.055 | 0.432 | 0.840 |
| GREY4.LOF | Optifloat™ Grey | Pilkington North America | 3.880 | 9832 | Monolithic | Neither | 0.528 | 0.054 | 0.056 | 0.558 | 0.057 | 0.059 | 0.840 | 0.840 |
| OptiView3.LOF | OptiView™ on Clear | Pilkington North America | 3.170 | 9996 | Coated | Front | 0.829 | 0.060 | 0.065 | 0.908 | 0.057 | 0.059 | 0.404 | 0.840 |
| OptiView4.LOF | OptiView™ on Clear | Pilkington North America | 3.810 | 9997 | Coated | Front | 0.832 | 0.058 | 0.058 | 0.917 | 0.052 | 0.052 | 0.452 | 0.840 |
| OptiView6.LOF | OptiView™ on Clear | Pilkington North America | 5.830 | 9998 | Coated | Front | 0.815 | 0.058 | 0.061 | 0.911 | 0.056 | 0.059 | 0.492 | 0.840 |
| OptiView8.LOF | OptiView™ on Clear | Pilkington North America | 7.900 | 9999 | Coated | Front | 0.724 | 0.054 | 0.058 | 0.891 | 0.051 | 0.055 | 0.460 | 0.840 |