Peer review VIR v105

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| VS1-08-6.VIR | VS08 on Clear | Viracon | 5.660 | 6445 | Coated | Back | 0.069 | 0.359 | 0.481 | 0.086 | 0.423 | 0.369 | 0.840 | 0.355 |