Peer review CIG v107

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LoE340+-2.CIG | LoE 340+ on 2mm Clear | Cardinal Glass Industries | 2.200 | 2138 | Coated | Back | 0.162 | 0.421 | 0.475 | 0.433 | 0.112 | 0.038 | 0.840 | 0.027 |
| LoE340+-3.CIG | LoE 340+ on 3mm Clear | Cardinal Glass Industries | 3.100 | 2139 | Coated | Back | 0.161 | 0.402 | 0.475 | 0.431 | 0.112 | 0.038 | 0.840 | 0.027 |
| LoE340+-4.CIG | LoE 340+ on 4mm Clear | Cardinal Glass Industries | 3.900 | 2140 | Coated | Back | 0.160 | 0.384 | 0.475 | 0.429 | 0.111 | 0.038 | 0.840 | 0.027 |
| LoE340+-5.CIG | LoE 340+ on 5mm Clear | Cardinal Glass Industries | 4.700 | 2141 | Coated | Back | 0.159 | 0.367 | 0.475 | 0.427 | 0.111 | 0.038 | 0.840 | 0.027 |
| LoE340+-6.CIG | LoE 340+ on 6mm Clear | Cardinal Glass Industries | 5.700 | 2142 | Coated | Back | 0.157 | 0.341 | 0.475 | 0.424 | 0.109 | 0.037 | 0.840 | 0.027 |
| LoE340+-8.CIG | LoE 340+ on 8mm Clear | Cardinal Glass Industries | 7.800 | 2143 | Coated | Back | 0.154 | 0.296 | 0.475 | 0.419 | 0.110 | 0.038 | 0.840 | 0.027 |