Peer review SFG v107

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SisecamDuosol_T50_One_6mm.sfg | Sisecam Duosol T 50 One 6mm | Sisecam Flat Glass | 5.800 | 25562 | Coated | Front | 0.245 | 0.505 | 0.377 | 0.557 | 0.075 | 0.137 | 0.025 | 0.844 |