Peer review VTA v107

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BirdSmart(1)SB90(2)CLR_6.VTA | BirdSmart™ (1) Solarban® 90 (2) Clear 6mm | Vitro formerly PPG | 5.664 | 5443 | Coated | Both | 0.215 | 0.366 | 0.602 | 0.569 | 0.094 | 0.134 | 0.838 | 0.023 |
| BirdSmart(1)SB90(2)ACU_6.VTA | BirdSmart™ (1) Solarban® 90 (2) Acuity® 6mm | Vitro formerly PPG | 5.664 | 5444 | Coated | Both | 0.223 | 0.475 | 0.603 | 0.580 | 0.096 | 0.134 | 0.838 | 0.023 |
| BirdSmart(1)SB90(2)STR_6.VTA | BirdSmart™ (1) Solarban® 90 (2) Starphire® 6mm | Vitro formerly PPG | 5.664 | 5445 | Coated | Both | 0.225 | 0.534 | 0.603 | 0.585 | 0.097 | 0.134 | 0.838 | 0.023 |