Peer review GRD v107

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CG62 5mmCLR090SG5mmCLR.grd | ClimaGuard 62-C5(2)/SGP-2.28/C5 | Guardian | 11.532 | 26301 | Laminate | Neither | 0.221 | 0.448 | 0.326 | 0.587 | 0.168 | 0.178 | 0.840 | 0.840 |
| CG70 5mmCLR090SG5mmCLR.grd | ClimaGuard® 70-C5(2)/SGP-2.28/C5 | Guardian | 11.532 | 26302 | Laminate | Neither | 0.276 | 0.403 | 0.294 | 0.630 | 0.184 | 0.182 | 0.840 | 0.840 |
| CG62 5mmCLR090SG5mmGRY.grd | ClimaGuard 62-C5(2)/SGP-2.28/Gy5 | Guardian | 11.532 | 26303 | Laminate | Neither | 0.128 | 0.445 | 0.147 | 0.332 | 0.157 | 0.087 | 0.840 | 0.840 |
| CG70 5mmCLR090SG5mmGRY.grd | ClimaGuard® 70-C5(2)/SGP-2.28/Gy5 | Guardian | 11.532 | 26304 | Laminate | Neither | 0.163 | 0.399 | 0.133 | 0.357 | 0.172 | 0.088 | 0.840 | 0.840 |
| CG62 3mmCLR090PVB_ATGCLR.grd | ClimaGuard 62-C3(2)/PVB-2.28mm/ATG | Guardian | 5.969 | 26444 | Laminate | Neither | 0.235 | 0.490 | 0.501 | 0.615 | 0.170 | 0.189 | 0.840 | 0.840 |
| CG70 3mmCLR090PVB_ATGCLR.grd | ClimaGuard® 70-C3(2)/PVB-2.28mm/ATG | Guardian | 5.969 | 26445 | Laminate | Neither | 0.304 | 0.440 | 0.449 | 0.661 | 0.187 | 0.193 | 0.840 | 0.840 |
| CG62 3mmCLR090SGP_ATGCLR.grd | ClimaGuard® 62-C3(2)/SGP-2.28mm/ATG | Guardian | 5.969 | 26446 | Laminate | Neither | 0.230 | 0.489 | 0.407 | 0.602 | 0.170 | 0.183 | 0.840 | 0.840 |
| CG70 3mmCLR090SGP_ATGCLR.grd | ClimaGuard® 70-C3(2)/SGP-2.28mm/ATG | Guardian | 5.969 | 26447 | Laminate | Neither | 0.293 | 0.439 | 0.366 | 0.647 | 0.186 | 0.187 | 0.840 | 0.840 |
| CG62 3mmGy090PVB_ATGCLR.grd | ClimaGuard® 62-Gy3(2)/PVB-2.28mm/ATG | Guardian | 5.969 | 26448 | Laminate | Neither | 0.166 | 0.282 | 0.497 | 0.428 | 0.105 | 0.178 | 0.840 | 0.840 |
| CG70 3mmGy090PVB_ATGCLR.grd | ClimaGuard® 70-Gy3(2)/PVB-2.28mm/ATG | Guardian | 5.969 | 26449 | Laminate | Neither | 0.217 | 0.253 | 0.444 | 0.459 | 0.113 | 0.181 | 0.840 | 0.840 |
| CG62 3mmGy090SGP_ATGCLR.grd | ClimaGuard® 62-Gy3(2)/SGP-2.28mm/ATG | Guardian | 5.969 | 26450 | Laminate | Neither | 0.162 | 0.282 | 0.403 | 0.418 | 0.105 | 0.173 | 0.840 | 0.840 |
| CG70 3mmGy090SGP_ATGCLR.grd | ClimaGuard® 70-Gy3(2)/SGP-2.28mm/ATG | Guardian | 5.969 | 26451 | Laminate | Neither | 0.209 | 0.253 | 0.361 | 0.449 | 0.112 | 0.175 | 0.840 | 0.840 |
| CG62 5mmCLR090PVB_ATGCLR.grd | ClimaGuard® 62-C5(2)/PVB-2.28mm/ATG | Guardian | 7.620 | 26452 | Laminate | Neither | 0.232 | 0.449 | 0.500 | 0.611 | 0.169 | 0.189 | 0.840 | 0.840 |
| CG70 5mmCLR090PVB_ATGCLR.grd | ClimaGuard® 70-C5(2)/PVB-2.28mm/ATG | Guardian | 7.620 | 26453 | Laminate | Neither | 0.299 | 0.404 | 0.449 | 0.657 | 0.185 | 0.193 | 0.840 | 0.840 |
| CG62 5mmCLR090SGP_ATGCLR.grd | ClimaGuard® 62-C5(2)/SGP-2.28mm/ATG | Guardian | 7.620 | 26454 | Laminate | Neither | 0.228 | 0.449 | 0.407 | 0.598 | 0.168 | 0.182 | 0.840 | 0.840 |
| CG70 5mmCLR090SGP_ATGCLR.grd | ClimaGuard® 70-C5(2)/SGP-2.28mm/ATG | Guardian | 7.620 | 26455 | Laminate | Neither | 0.289 | 0.404 | 0.365 | 0.643 | 0.184 | 0.186 | 0.840 | 0.840 |
| CG62 5mmGY090PVB_ATGCLR.grd | ClimaGuard® 62-Gy5(2)/PVB-2.28mm/ATG | Guardian | 7.620 | 26456 | Laminate | Neither | 0.135 | 0.200 | 0.496 | 0.347 | 0.085 | 0.175 | 0.840 | 0.840 |
| CG70 5mmGY090PVB_ATGCLR.grd | ClimaGuard® 70-Gy5(2)/PVB-2.28mm/ATG | Guardian | 7.620 | 26457 | Laminate | Neither | 0.177 | 0.180 | 0.443 | 0.373 | 0.090 | 0.178 | 0.840 | 0.840 |
| CG62 5mmGY090SGP_ATGCLR.grd | ClimaGuard® 62-Gy5(2)/SGP-2.28mm/ATG | Guardian | 7.620 | 26458 | Laminate | Neither | 0.132 | 0.200 | 0.402 | 0.339 | 0.085 | 0.170 | 0.840 | 0.840 |
| CG70 5mmGY090SGP_ATGCLR.grd | ClimaGuard® 70-Gy5(2)/SGP-2.28mm/ATG | Guardian | 7.620 | 26459 | Laminate | Neither | 0.171 | 0.180 | 0.360 | 0.365 | 0.090 | 0.172 | 0.840 | 0.840 |
| CG62 6mmCLR090PVB_ATGCLR.grd | ClimaGuard® 62-C6(2)/PVB-2.28mm/ATG | Guardian | 8.611 | 26460 | Laminate | Neither | 0.231 | 0.426 | 0.500 | 0.609 | 0.168 | 0.189 | 0.840 | 0.840 |
| CG70 6mmCLR090PVB_ATGCLR.grd | ClimaGuard® 70-C6(2)/PVB-2.28mm/ATG | Guardian | 8.611 | 26461 | Laminate | Neither | 0.296 | 0.384 | 0.448 | 0.654 | 0.184 | 0.193 | 0.840 | 0.840 |
| CG62 6mmCLR090SGP_ATGCLR.grd | ClimaGuard® 62-C6(2)/SGP-2.28mm/ATG | Guardian | 8.611 | 26462 | Laminate | Neither | 0.226 | 0.426 | 0.407 | 0.596 | 0.167 | 0.182 | 0.840 | 0.840 |
| CG70 6mmCLR090SGP_ATGCLR.grd | ClimaGuard® 70-C6(2)/SGP-2.28mm/ATG | Guardian | 8.611 | 26463 | Laminate | Neither | 0.286 | 0.384 | 0.365 | 0.640 | 0.183 | 0.186 | 0.840 | 0.840 |
| CG62 6mmGY090PVB_ATGCLR.grd | ClimaGuard® 62-Gy6(2)/PVB-2.28mm/ATG | Guardian | 8.611 | 26464 | Laminate | Neither | 0.119 | 0.166 | 0.495 | 0.306 | 0.077 | 0.174 | 0.840 | 0.840 |
| CG70 6mmGY090PVB_ATGCLR.grd | ClimaGuard® 70-Gy6(2)/PVB-2.28mm/ATG | Guardian | 8.611 | 26465 | Laminate | Neither | 0.157 | 0.150 | 0.442 | 0.329 | 0.080 | 0.176 | 0.840 | 0.840 |
| CG62 6mmGY090SGP_ATGCLR.grd | ClimaGuard® 62-Gy6(2)/SGP-2.28mm/ATG | Guardian | 8.611 | 26466 | Laminate | Neither | 0.117 | 0.166 | 0.402 | 0.299 | 0.076 | 0.168 | 0.840 | 0.840 |
| CG70 6mmGY090SGP_ATGCLR.grd | ClimaGuard® 70-Gy6(2)/SGP-2.28mm/ATG | Guardian | 8.611 | 26467 | Laminate | Neither | 0.152 | 0.150 | 0.359 | 0.322 | 0.080 | 0.170 | 0.840 | 0.840 |