Peer review EFG v107

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DSR 1_6.EFG | Emicool DSR 1 6mm | Emirates Float Glass.LLC | 5.750 | 28719 | Coated | Back | 0.152 | 0.362 | 0.451 | 0.259 | 0.352 | 0.172 | 0.840 | 0.059 |
| Vision cool Neutral 67_6.EFG | Vision cool Neutral 67 6mm | Emirates Float Glass.LLC | 5.750 | 28733 | Coated | Back | 0.607 | 0.111 | 0.139 | 0.664 | 0.162 | 0.165 | 0.840 | 0.815 |
| VC Dark grey_6.EFG | Emicool Vision cool Dark Grey 6mm | Emirates Float Glass.LLC | 5.750 | 28734 | Coated | Back | 0.114 | 0.263 | 0.109 | 0.130 | 0.147 | 0.073 | 0.840 | 0.439 |
| NE 80_6.EFG | Emicool Plus T NE 80 6mm | Emirates Float Glass.LLC | 5.750 | 28763 | Coated | Back | 0.549 | 0.256 | 0.339 | 0.844 | 0.098 | 0.085 | 0.840 | 0.026 |
| NE 80_4.EFG | Emicool Plus T NE 80 4mm | Emirates Float Glass.LLC | 3.850 | 28764 | Coated | Back | 0.569 | 0.284 | 0.341 | 0.853 | 0.100 | 0.087 | 0.840 | 0.026 |
| NE 80_5.EFG | Emicool Plus T NE 80 5mm | Emirates Float Glass.LLC | 4.750 | 28765 | Coated | Back | 0.552 | 0.261 | 0.340 | 0.846 | 0.100 | 0.087 | 0.840 | 0.026 |
| NE 80_8.EFG | Emicool Plus T NE 80 8mm | Emirates Float Glass.LLC | 7.750 | 28769 | Coated | Back | 0.530 | 0.231 | 0.339 | 0.838 | 0.097 | 0.084 | 0.840 | 0.026 |
| NE 72_6.EFG | Emicool Plus T NE 72 6mm | Emirates Float Glass.LLC | 5.750 | 28770 | Coated | Back | 0.509 | 0.227 | 0.300 | 0.807 | 0.087 | 0.056 | 0.840 | 0.074 |
| NN 30SL_6.EFG | Emicool Sun T NN 30SL 6mm | Emirates Float Glass.LLC | 5.750 | 28771 | Coated | Back | 0.198 | 0.322 | 0.372 | 0.325 | 0.272 | 0.124 | 0.840 | 0.054 |
| Vistasol Clear 6mm.EFG | EFG Vistasol Clear 6mm | Emirates Float Glass.LLC | 5.750 | 28772 | Coated | Back | 0.666 | 0.184 | 0.215 | 0.681 | 0.272 | 0.286 | 0.840 | 0.834 |
| Vitracool Bronze_6mm.EFG | EFG Vitracool Bronze 6mm | Emirates Float Glass.LLC | 5.750 | 28773 | Coated | Back | 0.264 | 0.113 | 0.302 | 0.203 | 0.131 | 0.343 | 0.840 | 0.848 |
| Vitracool Clear_6mm.EFG | EFG Vitracool Clear 6mm | Emirates Float Glass.LLC | 5.750 | 28774 | Coated | Back | 0.455 | 0.205 | 0.284 | 0.371 | 0.274 | 0.340 | 0.840 | 0.848 |
| Vitracool Green_6mm.EFG | EFG Vitracool Green 6mm | Emirates Float Glass.LLC | 5.750 | 28775 | Coated | Back | 0.220 | 0.122 | 0.304 | 0.288 | 0.230 | 0.342 | 0.840 | 0.848 |
| Vitracool Grey_6mm.EFG | EFG Vitracool Grey 6mm | Emirates Float Glass.LLC | 5.750 | 28776 | Coated | Back | 0.240 | 0.091 | 0.278 | 0.184 | 0.104 | 0.333 | 0.840 | 0.848 |
| Emicool Guard_6.EFG | Emicool Guard 6mm | Emirates Float Glass.LLC | 5.750 | 28777 | Coated | Back | 0.043 | 0.424 | 0.481 | 0.058 | 0.478 | 0.318 | 0.840 | 0.276 |