Peer review SGG v107

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| COOL-LITE KN 125 II 6mm.SGG | SGG COOL-LITE KN 125 II 6mm | Saint-Gobain Glass | 6.000 | 20958 | Coated | Back | 0.180 | 0.290 | 0.329 | 0.268 | 0.217 | 0.105 | 0.840 | 0.085 |
| COOL-LITE KN 125 II 8mm.SGG | SGG COOL-LITE KN 125 II 8mm | Saint-Gobain Glass | 8.000 | 20959 | Coated | Back | 0.177 | 0.276 | 0.329 | 0.267 | 0.214 | 0.105 | 0.840 | 0.085 |
| COOL-LITE KBRZ 127 II 6mm.SGG | SGG COOL-LITE KBRZ 127 II 6mm | Saint-Gobain Glass | 6.000 | 21204 | Coated | Back | 0.180 | 0.309 | 0.376 | 0.300 | 0.180 | 0.111 | 0.840 | 0.043 |
| COOL-LITE KN 148 II 6mm.SGG | SGG COOL-LITE KN 148 II 6mm | Saint-Gobain Glass | 6.000 | 21220 | Coated | Back | 0.306 | 0.391 | 0.339 | 0.514 | 0.248 | 0.118 | 0.840 | 0.032 |
| COOL-LITE KS 154 6mm.SGG | SGG COOL-LITE KS 154 6mm | Saint-Gobain Glass | 6.000 | 21332 | Coated | Back | 0.328 | 0.324 | 0.366 | 0.532 | 0.257 | 0.123 | 0.840 | 0.050 |