Peer review XYG v107

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XETG0170_8C.XYG | XETG0170_8C | XYG Glass | 7.880 | 22641 | Coated | Back | 0.440 | 0.165 | 0.223 | 0.683 | 0.108 | 0.031 | 0.843 | 0.115 |