Peer review GLW v110

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 07t_Enlighten.GLW | 0.7 mm Enlighten Glass | Corning Incorporated | 0.700 | 22500 | Monolithic | Neither | 0.919 | 0.078 | 0.078 | 0.920 | 0.079 | 0.079 | 0.840 | 0.840 |
| 05t_Enlighten.GLW | 0.5 mm Enlighten Glass | Corning Incorporated | 0.500 | 22501 | Monolithic | Neither | 0.919 | 0.077 | 0.077 | 0.920 | 0.079 | 0.079 | 0.840 | 0.840 |