Peer review SMP v110

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Hidden-Substrate-122025.smp | Hidden-Substrate-122025 | SMP Corporation | 2.000 | 0 | Monolithic | Neither | 0.910 | 0.080 | 0.080 | 0.915 | 0.083 | 0.083 | 0.840 | 0.840 |
| SMP_DualReflective_05.smp | Dual Reflective 5% | SMP Corporation | 2.000 | 29300 | Applied Film | Back | 0.061 | 0.582 | 0.212 | 0.056 | 0.577 | 0.109 | 0.840 | 0.705 |
| SMP_DualReflective_15.smp | Dual Reflective 15% | SMP Corporation | 2.000 | 29301 | Applied Film | Back | 0.154 | 0.472 | 0.316 | 0.172 | 0.454 | 0.235 | 0.840 | 0.702 |
| SMP_DualReflective_25.smp | Dual Reflective 25% | SMP Corporation | 2.000 | 29302 | Applied Film | Back | 0.222 | 0.198 | 0.320 | 0.229 | 0.121 | 0.287 | 0.840 | 0.755 |
| SMP_DualReflective_35.smp | Dual Reflective 35% | SMP Corporation | 2.000 | 29303 | Applied Film | Back | 0.417 | 0.120 | 0.112 | 0.411 | 0.111 | 0.091 | 0.840 | 0.823 |
| SMP_SupremeCeramicIR_70.smp | Supreme Ceramic IR 70% DA | SMP Corporation | 2.000 | 29304 | Applied Film | Back | 0.419 | 0.065 | 0.063 | 0.741 | 0.084 | 0.083 | 0.840 | 0.848 |
| SMP_EclipseVision_15.smp | Eclipse Vision 15% | SMP Corporation | 2.000 | 29305 | Applied Film | Back | 0.170 | 0.129 | 0.283 | 0.153 | 0.079 | 0.261 | 0.840 | 0.749 |
| SMP_EclipseVision_25.smp | Eclipse Vision 25% | SMP Corporation | 2.000 | 29306 | Applied Film | Back | 0.274 | 0.130 | 0.198 | 0.262 | 0.092 | 0.181 | 0.840 | 0.772 |