Peer review SFG v110

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sisecam_ExtraClear_4mm.sfg | Sisecam Extra Clear 4mm | Sisecam Flat Glass | 4.000 | 25507 | Monolithic | Neither | 0.862 | 0.075 | 0.075 | 0.908 | 0.080 | 0.080 | 0.837 | 0.837 |
| Sisecam_ExtraClear_5mm.sfg | Sisecam Extra Clear 5mm | Sisecam Flat Glass | 5.000 | 25508 | Monolithic | Neither | 0.846 | 0.074 | 0.074 | 0.904 | 0.080 | 0.080 | 0.837 | 0.837 |
| Sisecam_ExtraClear_6mm.sfg | Sisecam Extra Clear 6mm | Sisecam Flat Glass | 6.000 | 25509 | Monolithic | Neither | 0.837 | 0.074 | 0.074 | 0.902 | 0.079 | 0.079 | 0.837 | 0.837 |
| Sisecam_ExtraClear_8mm.sfg | Sisecam Extra Clear 8mm | Sisecam Flat Glass | 8.000 | 25510 | Monolithic | Neither | 0.807 | 0.071 | 0.071 | 0.896 | 0.078 | 0.078 | 0.837 | 0.837 |
| Sisecam_ExtraClear_10mm.sfg | Sisecam Extra Clear 10 mm | Sisecam Flat Glass | 10.000 | 25511 | Monolithic | Neither | 0.783 | 0.069 | 0.069 | 0.891 | 0.077 | 0.077 | 0.837 | 0.837 |
| SisecamProsolT60One_EC_6mm.sfg | Sisecam Prosol T 60 One 6mm | Sisecam Flat Glass | 6.000 | 25569 | Coated | Front | 0.360 | 0.490 | 0.345 | 0.764 | 0.084 | 0.096 | 0.031 | 0.844 |
| SisecamEcosol_T40_DB_6mm.sfg | Sisecam Ecosol T 40 Deep Blue 6mm | Sisecam Flat Glass | 6.000 | 25570 | Coated | Front | 0.247 | 0.450 | 0.151 | 0.406 | 0.237 | 0.164 | 0.061 | 0.844 |
| Sisecam_Green_6mm.sfg | Sisecam Green 6mm | Sisecam Flat Glass | 6.000 | 25571 | Monolithic | Neither | 0.395 | 0.053 | 0.053 | 0.713 | 0.068 | 0.068 | 0.837 | 0.837 |
| Sisecam_Grey_4mm.sfg | Sisecam Grey 4mm | Sisecam Flat Glass | 4.000 | 25572 | Monolithic | Neither | 0.594 | 0.060 | 0.060 | 0.577 | 0.061 | 0.061 | 0.837 | 0.837 |
| Sisecam_Grey_6mm.sfg | Sisecam Grey 6mm | Sisecam Flat Glass | 6.000 | 25573 | Monolithic | Neither | 0.482 | 0.056 | 0.056 | 0.453 | 0.056 | 0.056 | 0.837 | 0.837 |
| Sisecam_Grey_8mm.sfg | Sisecam Grey 8mm | Sisecam Flat Glass | 8.000 | 25574 | Monolithic | Neither | 0.390 | 0.052 | 0.052 | 0.356 | 0.052 | 0.052 | 0.837 | 0.837 |
| Sisecam_Bronze_4mm.sfg | Sisecam Bronze 4mm | Sisecam Flat Glass | 4.000 | 25575 | Monolithic | Neither | 0.612 | 0.063 | 0.063 | 0.630 | 0.065 | 0.065 | 0.837 | 0.837 |
| Sisecam_Bronze_5mm.sfg | Sisecam Bronze 5mm | Sisecam Flat Glass | 5.000 | 25576 | Monolithic | Neither | 0.552 | 0.060 | 0.060 | 0.569 | 0.062 | 0.062 | 0.837 | 0.837 |
| Sisecam_Bronze_6mm.sfg | Sisecam Bronze 6mm | Sisecam Flat Glass | 6.000 | 25577 | Monolithic | Neither | 0.497 | 0.057 | 0.057 | 0.513 | 0.059 | 0.059 | 0.837 | 0.837 |
| Sisecam_Bronze_8mm.sfg | Sisecam Bronze 8mm | Sisecam Flat Glass | 8.000 | 25578 | Monolithic | Neither | 0.408 | 0.053 | 0.053 | 0.425 | 0.055 | 0.055 | 0.837 | 0.837 |
| Sisecam_Bronze_10mm.sfg | Sisecam Bronze 10mm | Sisecam Flat Glass | 10.000 | 25579 | Monolithic | Neither | 0.328 | 0.046 | 0.046 | 0.342 | 0.047 | 0.047 | 0.837 | 0.837 |
| SisecamEcosol_T40_DG_6mm.sfg | Sisecam Ecosol T 40 Deep Green 6mm | Sisecam Flat Glass | 6.000 | 25580 | Coated | Front | 0.263 | 0.474 | 0.273 | 0.435 | 0.237 | 0.373 | 0.037 | 0.844 |