Peer review WHG v110

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6mmZD48 on clear.WHG | 6mmZD48 on clear | BEIJING WUHUATIANBAO GLASS CO.,LTD | 5.940 | 17460 | Coated | Back | 0.264 | 0.152 | 0.440 | 0.497 | 0.067 | 0.164 | 0.840 | 0.049 |