Peer review LOF v110

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| EnAdvLE1.6.LOF | Energy Advantage™ Low-E | Pilkington North America | 1.550 | 9900 | Coated | Front | 0.759 | 0.128 | 0.123 | 0.845 | 0.116 | 0.109 | 0.217 | 0.846 |