Peer review SGG v110

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PLT UN II INDIA 8mm.SGG | SGG PLANITHERM ULTRA N II INDIA 8mm | Saint-Gobain Glass | 8.000 | 20838 | Coated | Front | 0.581 | 0.307 | 0.241 | 0.874 | 0.052 | 0.064 | 0.046 | 0.840 |
| PLT UN II INDIA 10mm.SGG | SGG PLANITHERM ULTRA N II INDIA 10mm | Saint-Gobain Glass | 10.000 | 20839 | Coated | Front | 0.552 | 0.306 | 0.208 | 0.859 | 0.050 | 0.064 | 0.047 | 0.840 |
| CL XTREME 51-23 II DIA 8mm.SGG | SGG COOL-LITE XTREME 51-23 II DIAMANT 8mm | Saint-Gobain Glass | 8.000 | 20858 | Coated | Back | 0.195 | 0.371 | 0.604 | 0.562 | 0.105 | 0.118 | 0.840 | 0.021 |
| COOL-LITE SKN 175 II 8mm.SGG | SGG COOL-LITE SKN 175 II 8mm | Saint-Gobain Glass | 8.000 | 21093 | Coated | Back | 0.317 | 0.369 | 0.516 | 0.763 | 0.095 | 0.086 | 0.840 | 0.026 |
| PLANISTAR SUN PLUS 6mm.SGG | SGG PLANISTAR SUN PLUS 6mm | Saint-Gobain Glass | 6.000 | 21128 | Coated | Back | 0.342 | 0.399 | 0.495 | 0.768 | 0.081 | 0.082 | 0.840 | 0.027 |
| CL XTREME 51-23 II 8mm.SGG | SGG COOL-LITE XTREME 51-23 II 8mm | Saint-Gobain Glass | 8.000 | 21153 | Coated | Back | 0.191 | 0.322 | 0.604 | 0.554 | 0.103 | 0.118 | 0.840 | 0.021 |
| CL XTREME 51-23 DIA 6mm.SGG | SGG COOL-LITE XTREME 51-23 DIAMANT 6mm | Saint-Gobain Glass | 6.000 | 21172 | Coated | Back | 0.202 | 0.446 | 0.582 | 0.563 | 0.105 | 0.118 | 0.840 | 0.021 |
| COOL-LITE KN 166 II 4mm.SGG | SGG COOL-LITE KN 166 II 4mm | Saint-Gobain Glass | 4.000 | 21223 | Coated | Front | 0.382 | 0.480 | 0.382 | 0.667 | 0.208 | 0.200 | 0.029 | 0.840 |
| COOL-LITE KN 166 II 10mm.SGG | SGG COOL-LITE KN 166 II 10mm | Saint-Gobain Glass | 10.000 | 21226 | Coated | Front | 0.355 | 0.480 | 0.324 | 0.650 | 0.209 | 0.179 | 0.024 | 0.840 |
| CL ST Bright Silver 4mm.SGG | COOL-LITE ST Bright Silver 4mm | Saint-Gobain Glass | 4.000 | 21227 | Coated | Front | 0.713 | 0.239 | 0.239 | 0.682 | 0.310 | 0.310 | 0.845 | 0.840 |