Peer review CSG v110

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SJ12-79_5.CSG | Double LowE on Clear | China Southern Glass (CSG) | 4.870 | 19598 | Coated | Back | 0.419 | 0.268 | 0.402 | 0.782 | 0.055 | 0.040 | 0.840 | 0.039 |