Peer review VTA v110

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CLR_090SG_SB70(4)LAM_6.VTA | 6mmClear_090SG_6mmSB70(4) | Vitro formerly PPG | 13.614 | 25364 | Laminate | Back | 0.245 | 0.198 | 0.583 | 0.686 | 0.085 | 0.068 | 0.838 | 0.018 |
| CLR_060SG_SB70(4)LAM_6.VTA | 6mmClear_060SG_6mmSB70(4) | Vitro formerly PPG | 12.852 | 25365 | Laminate | Back | 0.247 | 0.206 | 0.583 | 0.690 | 0.086 | 0.068 | 0.838 | 0.018 |
| CLR_090PVB_SB70(4)LAM_6.VTA | 6mmClear_090PVB_6mmSB70(4) | Vitro formerly PPG | 13.614 | 25366 | Laminate | Back | 0.246 | 0.199 | 0.583 | 0.693 | 0.086 | 0.068 | 0.838 | 0.018 |
| CLR_060PVB_SB70(4)LAM_6.VTA | 6mmClear_060PVB_6mmSB70(4) | Vitro formerly PPG | 12.852 | 25367 | Laminate | Back | 0.248 | 0.206 | 0.583 | 0.694 | 0.086 | 0.068 | 0.838 | 0.018 |
| SB Champane Clear_6.VTA | Solarban Champane™ on Clear 6mm | Vitro formerly PPG | 5.664 | 5165 | Coated | Back | 0.239 | 0.372 | 0.477 | 0.501 | 0.239 | 0.040 | 0.840 | 0.031 |
| SB Champane Clear_8.VTA | Solarban Champane™ on Clear 8mm | Vitro formerly PPG | 7.925 | 5166 | Coated | Back | 0.231 | 0.319 | 0.477 | 0.494 | 0.233 | 0.040 | 0.840 | 0.031 |
| SB Champane Clear_10.VTA | Solarban Champane™ on Clear 10mm | Vitro formerly PPG | 9.398 | 5167 | Coated | Back | 0.227 | 0.291 | 0.477 | 0.490 | 0.230 | 0.039 | 0.840 | 0.031 |
| SB Champane Acuity_6.VTA | Solarban Champane™ on Acuity® 6mm | Vitro formerly PPG | 5.664 | 5168 | Coated | Back | 0.251 | 0.472 | 0.478 | 0.511 | 0.247 | 0.040 | 0.840 | 0.031 |
| SB Champane Acuity_8.VTA | Solarban Champane™ on Acuity® 8mm | Vitro formerly PPG | 7.925 | 5169 | Coated | Back | 0.247 | 0.439 | 0.478 | 0.508 | 0.245 | 0.040 | 0.840 | 0.031 |
| SB Champane Acuity_10.VTA | Solarban Champane™ on Acuity® 10mm | Vitro formerly PPG | 9.398 | 5170 | Coated | Back | 0.245 | 0.419 | 0.478 | 0.506 | 0.243 | 0.040 | 0.840 | 0.031 |
| SB Champane Starphire_6.VTA | Solarban Champane™ on Starphire® 6mm | Vitro formerly PPG | 5.664 | 5171 | Coated | Back | 0.256 | 0.532 | 0.478 | 0.514 | 0.250 | 0.040 | 0.840 | 0.031 |
| SB Champane Starphire_8.VTA | Solarban Champane™ on Starphire® 8mm | Vitro formerly PPG | 7.925 | 5172 | Coated | Back | 0.255 | 0.517 | 0.478 | 0.513 | 0.249 | 0.040 | 0.840 | 0.031 |
| SB Champane Starphire_10.VTA | Solarban Champane™ on Starphire® 10mm | Vitro formerly PPG | 9.398 | 5173 | Coated | Back | 0.254 | 0.507 | 0.478 | 0.512 | 0.248 | 0.040 | 0.840 | 0.031 |
| SB Champane Optigray_6.VTA | Solarban Champane™ on Optigray® 6mm | Vitro formerly PPG | 5.664 | 5174 | Coated | Back | 0.166 | 0.182 | 0.475 | 0.354 | 0.142 | 0.034 | 0.840 | 0.031 |
| SB Champane Optigray_8.VTA | Solarban Champane™ on Optigray® 8mm | Vitro formerly PPG | 7.925 | 5175 | Coated | Back | 0.140 | 0.129 | 0.474 | 0.304 | 0.116 | 0.032 | 0.840 | 0.031 |
| SB Champane Optigray_10.VTA | Solarban Champane™ on Optigray® 10mm | Vitro formerly PPG | 9.398 | 5176 | Coated | Back | 0.125 | 0.107 | 0.474 | 0.276 | 0.103 | 0.032 | 0.840 | 0.031 |
| SB Champane Solarbronze_6.VTA | Solarban Champane™ on Solarbronze® 6mm | Vitro formerly PPG | 5.664 | 5177 | Coated | Back | 0.146 | 0.191 | 0.474 | 0.298 | 0.115 | 0.032 | 0.840 | 0.031 |
| SB Champane Solarbronze_8.VTA | Solarban Champane™ on Solarbronze® 8mm | Vitro formerly PPG | 7.925 | 5178 | Coated | Back | 0.117 | 0.135 | 0.474 | 0.240 | 0.090 | 0.031 | 0.840 | 0.031 |
| SB65 Clear_5.VTA | Solarban® 65 on Clear 5mm | Vitro formerly PPG | 4.674 | 5338 | Coated | Back | 0.359 | 0.341 | 0.508 | 0.784 | 0.092 | 0.082 | 0.840 | 0.028 |
| SB65 Acuity_5.VTA | Solarban® 65 on Acuity® 5mm | Vitro formerly PPG | 4.674 | 5339 | Coated | Back | 0.373 | 0.426 | 0.509 | 0.797 | 0.094 | 0.083 | 0.840 | 0.028 |
| SB65 Starphire_5.VTA | Solarban® 65 on Starphire® 5mm | Vitro formerly PPG | 4.674 | 5340 | Coated | Back | 0.380 | 0.474 | 0.509 | 0.802 | 0.094 | 0.084 | 0.840 | 0.028 |
| SB65 Solarbronze_5.VTA | Solarban® 65 on Solarbronze® 5mm | Vitro formerly PPG | 4.674 | 5341 | Coated | Back | 0.241 | 0.199 | 0.502 | 0.514 | 0.064 | 0.066 | 0.840 | 0.028 |
| SB65 Solarbronze_6.VTA | Solarban® 65 on Solarbronze® 6mm | Vitro formerly PPG | 5.664 | 5342 | Coated | Back | 0.219 | 0.168 | 0.501 | 0.468 | 0.060 | 0.064 | 0.840 | 0.028 |
| SB65 Solarbronze_8.VTA | Solarban® 65 on Solarbronze® 8mm | Vitro formerly PPG | 7.925 | 5343 | Coated | Back | 0.175 | 0.120 | 0.500 | 0.377 | 0.054 | 0.060 | 0.840 | 0.028 |
| SB65 Solexia_6.VTA | Solarban® 65 on Solexia® 6mm | Vitro formerly PPG | 5.664 | 5344 | Coated | Back | 0.273 | 0.108 | 0.505 | 0.678 | 0.081 | 0.075 | 0.840 | 0.028 |
| SB65 Solexia_8.VTA | Solarban® 65 on Solexia® 8mm | Vitro formerly PPG | 7.925 | 5345 | Coated | Back | 0.243 | 0.080 | 0.503 | 0.634 | 0.076 | 0.072 | 0.840 | 0.028 |
| SB65 Azuria_6.VTA | Solarban® 65 on Azuria® 6mm | Vitro formerly PPG | 5.664 | 5350 | Coated | Back | 0.226 | 0.065 | 0.503 | 0.599 | 0.074 | 0.071 | 0.840 | 0.028 |
| SB65 Azuria_8.VTA | Solarban® 65 on Azuria® 8mm | Vitro formerly PPG | 7.925 | 5351 | Coated | Back | 0.195 | 0.057 | 0.502 | 0.535 | 0.068 | 0.067 | 0.840 | 0.028 |
| SB65 Optiblue_5.VTA | Solarban® 65 on Optiblue® 5mm | Vitro formerly PPG | 4.674 | 5352 | Coated | Back | 0.290 | 0.283 | 0.504 | 0.599 | 0.072 | 0.070 | 0.843 | 0.028 |
| SB65 Optiblue_6.VTA | Solarban® 65 on Optiblue® 6mm | Vitro formerly PPG | 5.664 | 5353 | Coated | Back | 0.274 | 0.253 | 0.504 | 0.563 | 0.069 | 0.068 | 0.840 | 0.028 |
| SB65 Optiblue_8.VTA | Solarban® 65 on Optiblue® 8mm | Vitro formerly PPG | 7.925 | 5354 | Coated | Back | 0.240 | 0.199 | 0.502 | 0.488 | 0.063 | 0.065 | 0.840 | 0.028 |
| SB65 Optiblue_10.VTA | Solarban® 65 on Optiblue® 10mm | Vitro formerly PPG | 9.398 | 5355 | Coated | Back | 0.220 | 0.171 | 0.501 | 0.444 | 0.059 | 0.063 | 0.840 | 0.028 |
| SB65 Optigray_6.VTA | Solarban® 65 on Optigray® 6mm | Vitro formerly PPG | 5.664 | 5356 | Coated | Back | 0.248 | 0.154 | 0.503 | 0.553 | 0.068 | 0.068 | 0.840 | 0.028 |
| SB65 Optigray_8.VTA | Solarban® 65 on Optigray® 8mm | Vitro formerly PPG | 7.925 | 5357 | Coated | Back | 0.209 | 0.110 | 0.501 | 0.476 | 0.061 | 0.064 | 0.840 | 0.028 |
| SB65 Optigray_10.VTA | Solarban® 65 on Optigray® 10mm | Vitro formerly PPG | 9.398 | 5358 | Coated | Back | 0.187 | 0.091 | 0.500 | 0.431 | 0.058 | 0.062 | 0.840 | 0.028 |
| SB65 Solarblue_6.VTA | Solarban® 65 on Solarblue® 6mm | Vitro formerly PPG | 5.664 | 5359 | Coated | Back | 0.227 | 0.134 | 0.502 | 0.492 | 0.063 | 0.065 | 0.840 | 0.028 |
| SB65 Solarblue_8.VTA | Solarban® 65 on Solarblue® 8mm | Vitro formerly PPG | 7.925 | 5360 | Coated | Back | 0.186 | 0.095 | 0.501 | 0.406 | 0.057 | 0.061 | 0.840 | 0.028 |
| SB65 Solargray_5.VTA | Solarban® 65 on Solargray® 5mm | Vitro formerly PPG | 4.674 | 5361 | Coated | Back | 0.212 | 0.159 | 0.501 | 0.443 | 0.059 | 0.063 | 0.840 | 0.028 |
| SB65 Solargray_6.VTA | Solarban® 65 on Solargray® 6mm | Vitro formerly PPG | 5.664 | 5362 | Coated | Back | 0.187 | 0.131 | 0.500 | 0.391 | 0.055 | 0.061 | 0.840 | 0.028 |
| SB65 Solargray_8.VTA | Solarban® 65 on Solargray® 8mm | Vitro formerly PPG | 7.925 | 5363 | Coated | Back | 0.141 | 0.091 | 0.499 | 0.293 | 0.050 | 0.058 | 0.840 | 0.028 |
| SB65 Pacifica_6.VTA | Solarban® 65 on Pacifica® 6mm | Vitro formerly PPG | 5.664 | 5375 | Coated | Back | 0.160 | 0.067 | 0.500 | 0.372 | 0.055 | 0.060 | 0.840 | 0.028 |
| SB65 Pacifica_8.VTA | Solarban® 65 on Pacifica® 8mm | Vitro formerly PPG | 7.925 | 5376 | Coated | Back | 0.118 | 0.053 | 0.499 | 0.277 | 0.050 | 0.057 | 0.840 | 0.028 |