Peer review AST v110

| Filename | Product Name | Manufacturer | Thick. (mm) | ID | Type | Coated Side | Tsol | Rfsol | Rbsol | Tvis | Rfvis | Rbvis | ef | eb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AeroShield7Air.AST | AeroShield 4mm on 3mm clear in air | AeroShield | 7.000 | 29210 | Coated | Back | 0.838 | 0.071 | 0.074 | 0.897 | 0.077 | 0.081 | 0.849 | 0.678 |
| AeroShield7Argon.AST | AeroShield 4mm on 3mm clear in argon | AeroShield | 7.000 | 29211 | Coated | Back | 0.838 | 0.071 | 0.074 | 0.897 | 0.077 | 0.081 | 0.849 | 0.678 |